| S/N | TEST | DESCRIPTIONS OF PROCEDURE |
| --- | --- | --- |
|  | DESCRIPTION | Determine the colour and appearance of material |
|  | SOLUBILITY | Determine its solubility in water and dilute acids. |
|  | IDENTIFICATION | A.Bulk density. The bulk density of a powder is the ratio of the mass of an untapped powder sample to its volume, including the contribution of the interparticulate void volume. Hence, the bulk density depends on both the density of powder particles and the spatial arrangement of particles in the powder bed. The bulk density is expressed in grams per millilitre despite the International Unit being kilogram per cubic metre (1 g/mL = 1000 kg/m3), because the measurements are made using cylinders. It may also be expressed in grams per cubic centimetre. B.It gives the reaction of carbonates. Introduce into a test-tube 0.1 g of the substance to be examined and suspend in 2 mL of water R or use 2 mL of the prescribed solution. Add 3 mL of dilute acetic acid R. Close the tube immediately using a stopper fitted with a glass tube bent twice at right angles. The solution or the suspension becomes effervescent and gives off a colourless and odourless gas. Heat gently and collect the gas in 5 mL of barium hydroxide solution R. A white precipitate is formed that dissolves on addition of an excess of hydrochloric acid R1. C.Dissolve about 15 mg in 2 mL of dilute nitric acid R and neutralise with dilute sodium hydroxide solution R. |
|  | APPEARANCE OF SOULTION | ### Solution S Dissolve 5.0 g in 100 mL of dilute acetic acid R. When the effervescence has ceased, boil for 2 min, allow to cool and dilute to 100 mL with dilute acetic acid R. Filter, if necessary, through a previously ignited and tared porcelain or silica filter crucible of suitable porosity to give a clear filtrate. |
|  | SOLUBLE SUBSTANCES | Mix 2.00 g with 100 mL of water R and boil for 5 min. Filter whilst hot through a sintered-glass filter (40) (2.1.2), allow to cool and dilute to 100 mL with water R. Evaporate 50 mL of the filtrate to dryness and dry at 100-105 °C. The residue weighs a maximum of 10 mg. |
|  | SUBSTANCES INSOLUBLE IN ACETIC ACID | Any residue obtained during the preparation of solution S, washed, dried and ignited at 600 ± 50 °C, weighs a maximum of 2.5 mg. |
|  | CHLORIDES | Dilute 1.5 mL of solution S to 15 mL with water R. To 15 mL of the prescribed solution add 1 mL of dilute nitric acid R and pour the mixture as a single addition into a test-tube containing 1 mL of silver nitrate solution R2. Prepare a standard in the same manner using 10 mL of chloride standard solution (5 ppm Cl) R and 5 mL of water R. Examine the tubes laterally against a black background. After standing for 5 min protected from light, any opalescence in the test solution is not more intense than that in the standard. |
|  | SULFATES | Dilute 1 mL of solution S to 15 mL with distilled water R. All solutions used for this test must be prepared with distilled water R. Add 3 mL of a 250 g/L solution of barium chloride R to 4.5 mL of sulfate standard solution (10 ppm SO4) R1. Shake and allow to stand for 1 min. To 2.5 mL of this suspension add 15 mL of the prescribed solution and 0.5 mL of acetic acid R. Prepare a standard in the same manner using 15 mL of sulfate standard solution (10 ppm SO4) R instead of the prescribed solution. After 5 min, any opalescence in the test solution is not more intense than that in the standard. |
|  | ARSENIC | Determined on 10 mL of solution S. Introduce the prescribed quantity of the substance to be examined into a test-tube containing 4 mL of hydrochloric acid R and about 5 mg of potassium iodide R and add 3 mL of hypophosphorous reagent R. Heat the mixture on a water-bath for 15 min, shaking occasionally. Prepare a standard in the same manner, using 0.5 mL of arsenic standard solution (10 ppm As) R. After heating on the water-bath, any colour in the test solution is not more intense than that in the standard. |
|  | CALCIUM | Dilute 2.6 mL of solution S to 150 mL with distilled water R. 15 mL of the solution complies with the test. All solutions used for this test are prepared with distilled water R. To 0.2 mL of alcoholic calcium standard solution (100 ppm Ca) R add 1 mL of ammonium oxalate solution R. After 1 min add a mixture of 1 mL of dilute acetic acid R and 15 mL of the prescribed solution or of a solution containing the prescribed quantity of the substance to be examined, and shake. Prepare a standard in the same manner using a mixture of 10 mL of aqueous calcium standard solution (10 ppm Ca) R, 1 mL of dilute acetic acid R and 5 mL of distilled water R. After 15 min, any opalescence in the test solution is not more intense than that in the standard. |
|  | IRON | Dissolve 0.1 g in 3 mL of dilute hydrochloric acid R and dilute to 10 mL with water R. Dilute 2.5 mL of this solution to 10 mL with water R. Dissolve the prescribed quantity of the substance to be examined in water R and dilute to 10 mL with the same solvent or use 10 mL of the prescribed solution. Add 2 mL of a 200 g/L solution of citric acid monohydrate R and 0.1 mL of thioglycollic acid R. Mix, make alkaline with ammonia R and dilute to 20 mL with water R. Prepare a standard in the same manner, using 10 mL of iron standard solution (1 ppm Fe) R. After 5 min, any pink colour in the test solution is not more intense than that in the standard. |
|  | ASSAY | Dissolve 0.150 g in a mixture of 2 mL of dilute hydrochloric acid R and 20 mL of water R. Carry out the complexometric titration of magnesium : Introduce the prescribed solution into a 500 mL conical flask and dilute to 300 mL with water R. Add 10 mL of ammonium chloride buffer solution pH 10.0 R and about 50 mg of mordant black 11 triturate R. Heat to about 40 °C then titrate at this temperature with 0.1 M sodium edetate until the colour changes from violet to full blue. 1 mL of 0.1 M sodium edetate is equivalent to 2.431 mg of Mg. 1 mL of 0.1 M sodium edetate is equivalent to 4.030 mg of MgO. |
|  | MICROBIAL ENUMERATION TEST | Determination of total aerobic microbial count (TAMC) and total combined yeasts and molds count (TYMC) by the pour plate method. - Slightly open the lid of the petri plate and dispense 1 ml of diluted sample in the center of the Petri plate using a sterile calibrated pipette. - Open the lid of the prepared media. (soya bean digest agar for TAMC and Sabouraud Dextrose Agar for TYMC) - Pour about 15-20ml of the sterilized molten media at the appropriate temperature above the sample. - Close the lid of the plate then mix the sample in the media properly by gently swirling the plate. The plate is generally swirled in an “S” or “8” shape. - Allow the media to completely solidify. - Simultaneously perform the negative control by plating 1ml of diluent used instead of the sample for each medium. - Incubate the plate in an inverted position under suitable incubation conditions (For TAMC Incubate the plates of Soybean Casein Digest Agar at 30°C-35°C for 48hours and For TYMC incubate the plates of Sabouraud Dextrose Agar at 20°C - 25°C for 72hours Test for Absence of Pathogen Test for E. coli: Using same dilution - Transfer 1ml of the sample into a sterile McCartney bottle containing 9ml of sterile MacConkey broth. - Incubate the MacConkey broth bottle at 300C-350C for 24 hours. - After incubation shake the tube and transfer loop full portion of MacConkey broth on the surface of the pre incubated Eosin Methylene Blue Agar petri plate. - Incubate plates at 30°C to 35°C for 48 hours. - For negative control, proceeding same as above except without sample, streak a portion of incubated sterile MacConkey broth medium on the surface of pre incubated Eosin Methylene Blue Agar. - Observe and record the presence or absence of specified microorganisms. - Include positive and negative controls in each batch of tests. - Verify the performance of media and reagents used in the analysis. Interpretation of Results - The bacterial count should not exceed 102cfu/ml while that of the fungal count should not be more than 102cfu/ml. There should be absence of fecal coliform (E coli). - If growth occurs in the negative control plate, the test is invalid, failed negative control must be investigated - The total aerobic microbial count (TAMC) is considered to be equal to the number of CFU found using casein soya bean digest agar; if colonies of fungi are detected on this medium, they are counted as part of TAMC. - The total combined yeasts/mould count (TYMC) is considered to be equal to the number of CFU found using Sabouraud dextrose agar; if colonies of bacteria are detected on this medium, they are counted as part of TYMC - When an acceptance criterion for microbiological quality is prescribed it is interpreted as follows: 101 CFU : maximum acceptable count＝20 102 CFU: maximum acceptable count＝200, 103 CFU: maximum acceptable count＝2000. |

| - CURRENT REVISION | - SUPERSEDE | - REASON FOR REVIEW |
| --- | --- | --- |
| - 00 | - NIL | - FIRST ISSUE |
| - 01 | - 00 | - Review of the procedures - Change in header and footer format |